SPEC NOTE DESCRIPTION: This Section specifies QUIETZONE® PINK NEXT GEN™ and SELECTSOUND® FIBERGLAS® acoustic insulation products not specified in any other Section of the Specifications. Refer to pertinent related Sections for information regarding any acoustic/fire insulation product not described herein.

SPEC NOTE: This Section can be used to specify the requirements of Work described below. It may also be used as a guide reference for the inclusion of certain articles and paragraphs (i.e. environmental, product descriptions, installation methods) in other Sections pertaining to projects requiring board or blanket glass fibre acoustic insulation prescribed in this Section.

For additional information concerning these products, contact your regional technical representative or consult Owens Corning Canada’s web site at the following address: www.owenscorning.ca.

SPEC NOTE ENVIRONMENT: This Section specifies environmentally responsible material choices, including recycling and reuse options, and generally available disposal options. The inclusion of recycled content provides efficient use of natural resources and diverts materials from the waste system.

SPEC NOTE: The glass fibres that compose the bulk of Owens Corning’s   QUIETZONE® PINK NEXT GEN™ and SELECTSOUND® glass fibre acoustic insulation products are produced from used recycled glass containers and flat glass products. These recycled wastes originate from two sources:

“Post-consumer” waste from construction sites and consumer “blue boxes” that have been separated and reintroduced into the manufacturing process.

“Post-industrial” waste from manufacturers.

# General

## SECTION INCLUDES

SPEC NOTE: Select one or more locations to be insulated; suppress or add as required.

### Glass fibre acoustic insulation installed in the following locations:

#### Voids in (wood) (steel) stud partitions [and framing placed on each side of (concrete) (concrete masonry unit) walls].

#### Between [ceiling] [floor] [light steel] [wood] [engineered wood] joists.

### [Semi-exposed] [and] [exposed] black glass fibre acoustic insulation [blankets] [boards] installed in the following locations:

#### On concrete and concrete masonry unit walls.

#### On gypsum board partitions where a blanket acoustic insulation has been installed.

#### Above perforated suspended ceilings.

#### Above ceilings or under raised floors used as ventilation plenums.]

### Accessories required to apply and maintain insulation in place.

## RELATED SECTIONS

SPEC NOTE: Select the appropriate Section or Sections directly pertaining to the following associated items.

### Section [06 10 00 –- Rough Carpentry]

### Section [07 21 16  –- Blanket Insulation]

### Section [07 21 26 –- Blown Insulation]

### Section [07 84 00 –- Firestopping]

### Section [07 92 00 –- Joint Sealing]

### Section [09 22 16 –- Non-structural Metal Framing]

### Section [09 51 13 –- Acoustical Panel Ceilings]

### Section [09 54 23 –- Linear Metal Ceilings]

### Section [09 84 00 –- Acoustic Room Components]

### Section [14 91 33 –- Linen Chutes]

### Section [14 91 82 –- Trash Chutes]

### Section [23 32 48 –- Acoustical Air Plenums]

## REFERENCES

SPEC NOTE: Edit list to suit standards specified in project specification.

### Underwriters' Laboratories of Canada (ULC):

#### CAN/ULC-S102:2018-REV1, Standard Method of Test for Surface Burning Characteristics of Building Materials and Assemblies

#### CAN/ULC-S102.2:2018-REV1, Standard Method of Test for Surface Burning Characteristics of Flooring, Floor Coverings and Miscellaneous Materials and Assemblies

#### CAN/ULC-S114:2018, Standard Method of Test for Determination of Non-Combustibility in Building Materials

#### CAN/ULC-S604:2016, Standard for Factory-Built Type A Chimneys

SPEC NOTE: CAN/ULC-S702 applies only to ECOTOUCH® QUIETZONE®, excluding thermal resistance properties.

#### CAN/ULC-S702.1:2014-AMD1, Standard for Mineral Fibre Thermal Insulation for Buildings, Part 1: Material Specification

### American Society for Testing and Materials International, (ASTM):

#### ASTM C165:2007 (2017) – Test for Measuring Compressive Properties of Thermal Insulations

#### ASTM C423:2017 – Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method

#### ASTM C553:2013(2019), Type 1 – Specification for Mineral Fiber Board Thermal Insulation for Commercial and Industrial Applications

#### ASTM C665:2017 – Standard Specification for Mineral Fiber Board Thermal Insulation for Light Frame Construction and Manufactured Housing

#### ASTM C1104:2019 – Test Method for Determining the Water Vapor Sorption of Unfaced Mineral Fiber Insulation

#### ASTM C1338:2019 – Standard Test Method for Determining Fungi Resistance of Insulation Materials and Facings

### Canadian Gas Association (CGAl):

#### CAN/CSA-B149.1:2020, Natural Gas and Propane Installation Code

#### CAN/CSA-B149.2:2020, Propane Storage and Handling Code

## SUBMITTALS

### Submit product data in accordance with Section [01 33 00 –- Submittal Procedures] [01 35 63 – Sustainability Certification Project Requirements].

### Certificates:

Owens Corning offer the following performance reports from National Research Council (NRC) of Canada:

- Summary Report for Consortium on Gypsum Board Walls: Sound Transmission Results, Internal Report IRC-IR-693

- Gypsum Board Walls: Transmission Loss Data, internal report No. IRC-IR-761

- Summary Report for Consortium on Floors: Sound Transmission Class and Impact Insulation Class Results, Internal Report IRC-IR-766

Additional testing laboratories include:

- Owens Corning Acoustic Laboratory (W & OC), Granville, Ohio & Acculab Consultants in Acoustics, Columbus, Ohio

- Riverbank Acoustic Laboratory (RAL)

#### Submit third party testing reports indicating compliance with specified performance.

#### Submit environmental certificates issued by independent agencies and the evaluation of the products' contribution towards obtaining LEED® Canada credits mentioned in article QUALITY ASSURANCE.

Visit www.owenscorning.ca for a current copy of the Safety Data Sheet (SDS/MSDS) for insulation products.

### Submit WHMIS SDS –-Safety Data Sheets in accordance with Section [01 35 63 – Sustainability Certification Project Requirements]. Indicate VOC content.

### Submit samples in accordance with Section [01 33 00 –-Submittal Procedures].

#### One sample of each type of insulation specified.

#### One [two] sample[s] of each type specified accessory and fastener.

## QUALITY ASSURANCE

### Identification: Clearly label each bag of insulation with the information listed in manufacturer’s applicable Product Data Sheet.

### Provide Products listed in:

#### Underwriters Laboratories of Canada (ULC): List of Equipment and Materials, Building Materials,

#### Underwriters Laboratories of Canada (ULC) : List of Equipment and Materials Fire Resistance.

#### Underwriters Laboratories Inc. (ULI) : Fire Resistance, Volume 1,

### Environmental certification by an independent agency:

SPEC NOTE: The GREENGUARD Environmental Institute (GEI) is a third-party, industry-independent, non-profit organization that certifies various characteristics of products submitted by manufacturers. The GEI oversees the GREENGUARD Certification Program to establish, among others, the low-emissivity of toxic chemical products and volatile particles from glass fibre acoustic insulation installed inside a building. Product performances are measured following standardized procedures, test methods, allowable emissions levels, product sample collection and handling, testing type and frequency, and program application processes and acceptance.

#### Submit the "GREENGUARD Standard for Low Emitting Products Certified" certificate issued by the GREENGUARD Environmental Institute (GEI) certifying that the prescribed acoustical blanket [and board] insulation meets low VOC emission requirements contained in the tested product; web site :www.greenguard.org.

SPEC NOTE: SCS (Scientific Certification Systems) is an independent third-party certification agency; originally, its role was to test for pesticide residues in fresh produce. The Environmental Claims Certification program was initiated by the SCS; this program’s objective is to measure the recycled materials content in manufactured products. When a submitted product meets the various procedures imposed by the program, the SCS issues a “Certificate of Achievement” for a limited duration. This certificate permits designers to confidently choose an Owens Corning manufactured acoustic insulation –- to add to accumulative credits in order to obtain the desired LEED Canada certification.

#### Submit the certificate issued by the Scientific Certification Systems (SCS) certifying that the prescribed acoustical batt [and board] insulation meets the minimum claimed recycled materials content; web site :www.scscertifed.com.

#### The certificates shall include the following details: certificate number, duration of the certification and all restrictions issued by the certification agency for the product[s], as applicable.

SPEC NOTE: For quite a few years now the Canada Green Building Council (CaGBC) has promoted the application of the LEED Green Building Rating System (LEED Canada NC and CS) in Canada. LEED is the acronym of Leadership in Energy and Environmental Design.

SPEC NOTE: As a design guideline and a third-party certification tool, LEED aims to improve occupant comfort, environmental performance and economical efficiency of buildings by the use of proven and innovative procedures, standards and technologies. It furnishes a definition generally recognized in the industry of what constitutes a “green building”. The LEED Green Building Rating System comprises a set of explicit performance criteria organized into seven (7) principal categories: Sustainable Sites, Water Efficiency, Energy and Atmosphere, Materials and Resources, Indoor Environmental Quality. Innovation in Design,  Regional Priority. This seventh category includes Durable Building Credit (formerly MR Credit 8) and a Regional Priority Credit which addresses geographically-specific environmental properties For each performance criteria, the LEED Rating System states the fundamental objective and the necessary documentation to be submitted to meet each compulsory condition and to obtain each voluntary “credit”. Projects are awarded one or more points for their certification by meeting or exceeding each credit’s technical requirements. All compulsory conditions must be met before the project may be admissible to the certification. The points are then accumulated into a final total corresponding to one of the possible LEED certification levels: CERTIFIED, SILVER, GOLD or PLATINUM.

SPEC NOTE: Indoor Air Quality (IAQ) LEED credits pertaining to low VOC emitting materials are awarded to adhesives, waterproofing mastics, composite wood products and carpeting systems but are not applicable to acoustic insulation.

### Contribution of the acoustic insulation to the LEED® certification of the building Project:

#### Categories and performance criteria to obtain credits, as established by the Canadian Green Building Council Rating System LEED® Canada NC and CS:

##### Materials and Resources (MR): credit 4 recycled content.

##### Materials and Resources (MR): credit 5  for locally or regionally produced materials.

##### Material Disclosure and Assessment (MR PC 61):  The intent is to increase the use of products and materials with life cycle, ingredients, and attributes understood and optimized to improve overall environmental, economic, and social performance.

##### Innovation & Design Process (ID): credit 1 dependent on effectiveness of innovation being applied;(the acoustical performance of glass fibre acoustic insulation is effective in reducing noise transfer through building assemblies).

### Sustainability Standards Certifications:

SPEC NOTE: Include the following paragraphs to list the product’s environmental qualities that are certified by third-party independent agencies. Owens Corning Canada product certificates from SCS Global Services (various forms and sizes) can be found at www.scscertified.com.

#### Acoustic Blanket Insulation For Cavities: Provide third party certificates attesting to the following post-industrial and post-consumer recycled materials content:

##### Average: 73% recycled content, conforming to Scientific Certification Systems Content Standard V7-0:

##### 9% “post-industrial” (or pre-consumer) recycled materials content; average for all North American manufacturing facilities;

##### 64% “post consumer” recycled materials content.

#### Surface Applied Acoustic Board and Blanket: Provide third party certificates attesting to the following post-industrial and post-consumer recycled materials content :

##### 57% (claimed by the manufacturer)

###### 52% “post-industrial” (or pre-consumer) recycled materials content

###### 5 % “post consumer” recycled materials content.

For up-to-date GREENGUARD Indoor Air Quality Certified Certification of Owens Corning PINK NEXT GEN™ FIBERGLAS® blanket thermal insulation, go to www.greenguard.org.

#### Provide third party certificates attesting to compliance with GREENGUARD Indoor Air Quality CertifiedSM standards:

##### GREENGUARD Product Emission Standard for Children & Schools:

###### Individual VOCs		< 1/100 TLV and < ½ CA chronic RE

###### Formaldehyde			< 0.0135 ppm/13.5 ppb

###### Total VOCs			< 0.22 mg/m³

###### Total Aldehydes		< 0.043 ppm/43 ppb

###### Total Phthalates		< 0.01 mg/m³

###### Total Particles (< 10µm) 	< 0.02 mg/m³

## DELIVERY, STORAGE AND HANDLING

### Deliver, store and handle glass fibre batts, blankets and boards in accordance with manufacturer's printed instructions.

### Store materials in their original packaging in a dry interior location.

### Protect materials from the weather and store at a temperature and a relative humidity recommended by the manufacturer.

### Separate waste materials for [reuse] [and] [recycling] in accordance with Section [01 74 19 –- Construction Waste Management and Disposal].

### Collect and separate [paper] [plastic] [polystyrene] [corrugated cardboard] packaging material [for disposal in appropriate on-site bins] [for recycling in accordance with Waste Management Plan].

### Safety: Comply with requirements of Workplace Hazardous Materials Information System (WHMIS) regarding use, handling, storage, and disposal of acoustic insulation materials.

### Protection

SPEC NOTE:  Specify protection when glass fibre acoustic insulation is applied in an enclosed area.

#### Ensure applicator's personnel wears protection equipment such as breathing masks (dust-proof type masks prescribed in Product Data Sheet), face and eye protection (safety goggles or eye glasses) and skin protection (gloves, long-sleeved shirts and pants).

#### Provide temporary enclosures to prevent dust from contaminating air beyond application area.

#### Protect adjacent surfaces and equipment from damage by fall-out and dust.

## AMBIENT CONDITIONS

### Apply acoustic insulation only when ambient climatic conditions (high humidity levels) and temperature of surfaces to be insulated are within acceptable limits to prevent risk of condensation.

# Products

SPEC NOTE: Use QUIETZONE® PINK NEXT GEN™ FIBERGLAS® Acoustic Insulation Blankets to fill wall, partition and floor and ceiling cavities to contribute to the assembly's soundproofing. For additional information, refer to Product Data Sheet 09 81 16.16.OCC NEXT GEN PINK™ QUIETZONE®. NEXT GEN PINK™ QUIETZONE® acoustic batts are non-combustible and ULC labeled.

Use QUIETZONE® PINK NEXT GEN™ FIBERGLAS® Acoustic Insulation blankets in ULC fire rated assemblies.

The ULC Fire Resistance Directory section under the title ‘’Walls and Partitions’’ states:

The wall and partition designs illustrated are identified by a design number and an hourly fire rating. With the exception of support (i.e. studs) and fastener (i.e. nails, screws) spacings, the dimensions given in the following designs are to be construed as the minimum allowable for each rated assembly. Support and fastener spacings are the maximum allowable.

Listed and labelled mineral thermal building insulation that is processed from rock and glass may be used only in ULC non-loadbearing wall assembly designs consisting of wallboard and steel or wood studs with a fire resistance rating not exceeding 2 hours when illustrated without insulation, without detracting from the rating assigned to the assembly.

The following ULC fire rated assemblies can be referenced with QUIETZONE® NEXT GEN PINK™ FIBERGLAS® Acoustic Insulation blankets filling the cavity:

ULC 407, 409  413, 453, 484 and 486 for a 45-minute to 1-hour fire rating non-load bearing wall with steel studs and listed gypsum board;

ULC  449, 453 and 454 for a 1- to 2- hour fire rating non-load bearing wall with steel studs and listed gypsum board.

## GLASS FIBRE ACOUSTIC INSULATION FOR CAVITIES IN PARTITIONS, [FURRED WALLS], CEILINGS [AND] FLOORS

### Glass Fibre Acoustic Blanket insulation:

#### To CAN/ULC-S702, type 1, pre-formed unfaced glass fibre batt acoustic insulation.

Refer to NBC 2015, tables A-9.10.3.1-A/-B and Product Data Sheet 09 8116.16.OCC QUIETZONE® PINK NEXT GEN™ for various assemblies contributing to acoustic performance and fire resistance.

#### STC contribution and fire resistance (hr): to National Building Code (NBC).

#### Surface burning characteristics to CAN/ULC-S102:

##### flame spread: 0

##### smoke developed: 0

#### Surface burning characteristics to CAN/ULC-S102.2:

##### flame spread: 0

##### smoke developed: 0

#### Smoulder resistance: Mass loss <= 0.02%, to ULC S-129.

#### Non-combustible: to CAN4-S114.

#### Formaldehyde-free formulation

#### Does not support mold growth: meets fungal resistance criteria in ASTM C1338

#### Non-corrosive: meets corrosion resistance criteria in ASTM C665

### Manufacturer: QUIETZONE® PINK NEXT GEN™ FIBERGLAS® Acoustic Blanket insulation manufactured by Owens Corning Canada.

SPEC NOTE: Use EcoTouch® SELECTSOUND® Black Acoustic Blanket in rooms where a high sound absorption and reverberation control is required, notably in museums, churches, multiplex cinemas, sound studios, performing arts centres, sports complexes and above metal suspended ceilings; for additional information, refer to

Product Data Sheet 09 81 16.16.OCC SELECTSOUND® Black Acoustic Blanket Insulation.

## GLASS FIBRE BLACK ACOUSTIC BLANKET INSULATION FOR SURFACE APPLICATION ON WALLS, (SUSPENDED CEILINGS) (AND) VENTILATION PLENUMS

### Glass Fibre Acoustic Blanket insulation:

#### To ASTM C553, Type III, pre-formed blanket acoustic insulation, black colour, faced with a black fibre glass mat.

SPEC NOTE: Refer to TABLE 2 –- Acoustic Performances in Product Data Sheet for STC at different frequencies.

#### Noise Reduction Coefficients to ASTM C423, (type A apparatus, on solid backing):

##### Thickness	Density		Noise Reduction Coefficient (NRC)

##### 25 mm (1 in.)	24 kg/m³ (1.5 lbs/ft³)		0.70

##### 51 mm (2 in.)	24 kg/m³ (1.5 lbs/ft³)		1.00

#### Surface burning characteristics to CAN/ULC-S102 and UL 723:

##### flame spread: 25

##### smoke developed: 50

### Colour: Black.

### Manufacturer:: SELECTSOUND® Black Acoustic Blanket insulation manufactured by Owens Corning.

SPEC NOTE: SELECTSOUND® Black Acoustic Board is used in the same applications as black acoustic blankets where higher compressive strength is required. For additional information, refer to

Product Data Sheet 09 81 13.16.OCC SELECTSOUND® Black Acoustic Board Insulation.

## GLASS FIBRE BLACK ACOUSTIC BOARD INSULATION FOR SURFACE APPLICATION ON WALLS, (AND SUSPENDED CEILINGS)

### Glass Fibre Acoustic Board Insulation:

#### Pre-formed semi-rigid fibre glass board acoustic insulation, black colour, faced with a black glass fibre mat.

### Nominal compressive strength: to ASTM C165:

#### at 10% deformation: 1197 Pa (25 lbs/ft2)

#### at 25% deformation: 4309 Pa (90 lbs/ft2)

SPEC NOTE: For specific applications and acoustical performance for the SELECTSOUND® Acoustic Board product refer to the Product Data Sheet 09 81.13.16.OCC SELECTSOUND® Black Acoustic Board Insulation.

### Noise Reduction Coefficients to ASTM C423, (type A apparatus, on solid backing):

#### Thickness	Density		Noise Reduction Coefficient (NRC)

#### 25 mm (1 in.)	48 kg/m³ (3.0 lbs/ft³)		0.70

#### 51 mm (2 in.)	48 kg/m³ (3.0 lbs/ft³)		1.00

### Surface burning characteristics to CAN/ULC-S102 and UL 723:

#### flame spread: 25

#### smoke developed: 50

### Colour: Black.

### Manufacturer: SELECTSOUND® Black Acoustic Board insulation manufactured by Owens Corning.]

## ACCESSORIES FOR BLACK ACOUSTIC BOARD AND BLANKET INSULATION

### Fasteners:

#### Stick clips: impaling type, supplied with [self-adhesive] [screw fastened] perforated 50 mm x 50 mm x 0.8 mm sheet steel base as recommended by manufacturer; with integral 2.5 mm diameter sharpened pin of appropriate length and minimum 25 mm diameter self-locking retainers.

### Adhesive: as recommended by manufacturer.

# Execution

## EXAMINATION

### Examine installation conditions and ensure:

#### Acoustic and firestop sealants required at [steel] [wood] stud framing [concrete masonry unit wall] junctions with adjacent building components or at mechanical and electrical conduit and duct penetrations are installed.

#### Mechanical, electrical [and] [telecommunications] service lines in walls [and] [ceilings][floors] to be insulated acoustically have been inspected.

#### Supports are dry and ready to receive the acoustic insulation.

### Do not commence installation until base work has been corrected and inspections completed.

## INSTALLATION - GENERAL

SPEC NOTE: Ensure resilient furring will be installed where specified.

### Coordinate acoustic insulation installation with gypsum board [  ] [metal resilient] [wood] [furring] installation on studs [and] [joists] at [400 mm (16 in.)] [600 mm (24 in.)].

### Do not compress acoustic insulation to fit voids.

SPEC NOTE: Ensure clearances meet local building safety regulations and code requirements. For electrical fixtures housed in a CSA-approved insulated enclosure, prescribed clearances are not required unless indicated otherwise by the fixture's manufacturer. Edit the following paragraph to suit.

### Keep insulation minimum 75 mm from heat-emitting devices, such as recessed light fixtures (which are not encased in thermally insulated boxes), and minimum 50 mm from sidewalls of chimneys as per CAN/ULC-S604 and CSA-B149.1 and CSA-B149.2 type B and L vents.

## INSTALLATION OF ACOUSTIC BLANKET INSULATION IN PARTITION, [FURRED WALL], CEILING [AND] FLOOR VOIDS

### Install acoustic blankets full width and length, with tight joints, between wall [ceiling] [floor] framing and around penetrating electrical service boxes, piping, air ducts and frames.

### Partitions, [furred concrete or concrete masonry unit walls]:

#### Place [__] thick acoustic blankets where indicated on the Drawings and to thickness required to obtain acoustic performance indicated for the assembly.

#### Place acoustic blankets between studs ensuring friction fit, free of sags, folds or open joints that may let sound pass through.

#### Install blankets from the bottom up, tightly adjusted and trim accurately with a utility knife.

### Ceilings, (floors):

#### Place [__] thick acoustic blankets where indicated on the Drawings and to thickness required to obtain acoustic performance indicated for the assembly.

#### Install acoustic blankets in full width and length between ceiling [floor] joists and adjust accurately, free of sags or open joints that may let sound pass through.

#### Overlap joints in multiple layer installations.]

SPEC NOTE: Verify with acoustic ceiling tile manufacturer if tile loading is permitted depending on installation conditions. Owens Corning can supply information on unit loads, as required.

#### Place [___] thick acoustic blankets above suspended ceiling tiles located [above offices and extending [2440 mm (8')] above adjacent open areas.]

#### Place [__] thick acoustic blankets where indicated on the Drawings and to thickness required to obtain acoustic/fire performance indicated for the assembly.]

## INSTALLATION OF BLACK BLANKET [AND BOARD] ACOUSTIC INSULATION ON WALLS, [SUSPENDED CEILINGS] [AND] [VENTILATION PLENUM]

### Carefully adjust acoustic blankets [and] [boards] horizontally and vertically.

#### Butt joints tightly between each blanket [and board] and around penetrating electrical service boxes, piping, air ducts and framing.

#### Where multiple layers are required, overlap all joints.

### Coordinate blanket [and] [board] installation with decorative perforated screen [suspended ceiling] installation prescribed in other Sections and used to hold the acoustic insulation in place.

### Vertical application:

#### Mechanical fastening: fasten acoustic blankets [boards] using minimum one (1) stick clip per 0.2 m2 (2 sq. ft); fasten stick clips to supports as per support manufacturer's instructions (screws or adhesive). Impale blankets [and] [boards] and lock in place with retainers. Cover protruding metal pins.

#### Adhesive fastening:

##### Permanent installation: adhere blankets [and] [boards] to prevent sagging once fastened.

##### Temporary installation: adhere blankets [and] [boards] temporarily until retained by a decorative screen or until mechanically fastened.

## CLEANING

### Upon completion of installation, remove surplus materials, rubbish, tools and safety barriers.

### Take all necessary precautions to keep acoustic insulation and its components clean. Immediately remove all dirt and stains.

END OF SECTION

OWENS CORNING CANADA LP

3450 McNicoll Avenue

Scarborough, Ontario  M1V 1Z5

Tel:  1 800 504-8294  Fax: 1 800 504-9698

salvatore.ciarlo@owenscorning.com

The colour PINK is a registered trademark of Owens Corning.  © 2021. Owens Corning. All Rights Reserved.  Publication # 200024F